I. GENERAL:

Scope of Work - Furnish all necessary materials for the complete installation of aluminum windows for this project as shown on the drawings and herein specified.  Windows shall be the "Series 1450" as manufactured by Thermal Windows, Inc., Tulsa, Oklahoma.  The "Series 1450" is a fixed lite picture window with thermally improved frame.  The specifications and materials for the "Series 1450" are as follows:

II. PRODUCTS:

Materials - Aluminum shall be of proper alloy for commercial window construction.  All extruded sections shall be of 6063-T5 aluminum alloy.

Frame - Main frame members shall be a nominal thickness as required by ANSI/AAMA 101.  Main frame shall be 3.250" in depth.  Main frames are to be extruded aluminum with a dual insulbar thermal barrier system creating a .625” wide thermal barrier.

III. CONSTRUCTION:

Assembly – Main frame shall be of mitered, sealed, crimped and staked corner construction. Each corner shall consist of one extruded aluminum corner key held in place with two die cast retainer pins, one die cast corner key staked in place and one friction fit hard plastic corner key.

Glazing – Glass shall be inside glazed using EPDM gasket at exterior perimeter with extruded aluminum glazing bead and EPDM wedge at interior of glass.  The insulated glass units shall be 1.000" overall thickness with two lites of .125” glass, separated by a .750" air space for optimum insulation.  All insulated glass units shall meet the requirements of the ASTM E 2188-02 / ASTM E 2190-02 specification, Class "A".

Finish - Shall be a factory applied baked polyurethane powder coat finish meeting the requirements of AAMA 2604 for Pigmented Organic Coating on Extruded Aluminum.  Standard Tier I colors available are bronze, white, crème, sandstone, and almond.  Bronze anodizing, clear anodizing and high performance AAMA 605.2 finishes are optional.

IV. PERFORMANCE:

Structural - Shall meet the requirements of ANSI/AAMA 101/I.S 2-97 F-HC40 specification.

V. INSTALLATION:

Qualifications - Only skilled mechanics with experience in this trade.  Units shall be installed plumb, level, square and shall be secured in accordance with detailed shop drawings.  A non-hardening sealant compatible with aluminum shall be provided by the installer and applied in sufficient quantity to provide a weathertight seal between the window and surrounding construction.

Installation Details - The window manufacturer shall submit complete installation details for the Architects approval.  The drawings shall show elevations of windows, full size details of frame and vents, details of construction and anchorage of window.